PRODUCT DATA SHEET & MATERIAL SAFETY DATA SHEET

Identification of the Chemical and the Origin

Product					: Glass Beads for Blasting

Origin						: China

Manufacturer of Material                    	:Oceanus Industrial International Limited

Composition and Information on dangerous ingredients

Chemical Composition ( % )

SiO2						: 73.00

Na2O						: 14.30

K2O						: 0.60

CaO						: 9.20

MgO						: 4.00

Fe2O3						: 0.11

Al2O3						: 2.00

SO3						: 0.30

Technical Properties

Soda Lime Glass				: No free silica

Specific Gravity				: 2.45-2.50 g /cm3

Bulk Density					: 1.54 kg / m3

Hardness 					: 5.5 MOHS

Color						: Clear / Colorless

Configuration					: Spherical

Roundness					: 65-95%

Available Sizes

| Size | No.3 | No.4 | No.6 | No.8 | No.9 | No.10 | No.11 | No.12 | No.13 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Microns | 425-850 | 250-425 | 180-300 | 150-250 | 106-212 | 75-150 | 53-106 | 45-90 | 45-0 |

Health Hazard Information

Health Effects

Swallowed					: None know

Eye						: Irritation may result if recommended exposure limits are

Exceeded

Skin						: None know

Inhaled						: Dust in excess of recommended exposure limits may result

In irritation of the respiratory tract.

First Aid

Swallowed					: None know

Eye						: Rinse with water

Skin						: None know

Inhaled						: Remove to fresh air

Advice to Doctor

Cronic lung conditions may be aggravated by exposure to high concerntration of dust.

Precautions for use

Exposure Limits				: Nuisance Dust

Ventilation					: Local exhaust recommended in case of dusting

Personal Protection				: Approved eye goggles & dust mask to be worn in dusty

Conditions

Flammable					: Non-flammable

Safe Handling Information

Storage and Transport				: Care should be taken to avoid dusting

Spills and Disposal				: Spillage may result in slippery conditions

Fire / Explosion Hazard			: None

Other Information				: (Material to avoid) – Hydrofluoric Acid

Use standard good manufacturing practices when handling

Material.

entilation	ust

use

ns may be aggravated by exposure to high concerntra